A352UP  – CL

TYPE II MACROPOROUS STRONG BASE ANION EXCHANGE RESIN

(Designed for use in de-ashing and high purity water applications)

Product Description

A352UP(CL) resin is a UNIFORM PARTICLE SIZE,  high capacity, macroporous polystyrene Type II strong base anion exchange resin.

Chiefly used in sugar refining with higher ion exchange capacity.

| Typical Physical, Chemical & Operating Characteristics |  |
| --- | --- |
| Polymer Structure | Polystyrene cross-linked with Divinylbenzene |
| Physical Form and Appearance | Tough white spherical beads |
| Whole Bead Count | 90% Min. |
| Functional Groups | R-N+(CH3)2(C2H4OH)OH- |
| Ionic Form (as shipped) | CL- |
| Shipping Weight, approx. | 680 g/l (42 lb./ft.3) |
| Particle Size (mm) | -0.5 mm, <5% +1.0 mm, <5% |
| Moisture retention, Cl- form | 47-57% |
| Swelling, Cl- to OH-, % | <15% |
| Total Capacity in Cl- form | >1.20 meq/ml |
| pH Range, Stability | 0–14 |

CHEMI	CAL AND THERMAL STABILITY

A352UP(CL) resin is insoluble in dilute or moderately concentrated acids, alkalies, and in all common solvents. However, exposure to significant amounts of free chlorine, “hypochlorite” ions, or other strong oxidizing agents over long periods of time will eventually break down the crosslinking. This will tend to increase the moisture retention of the resin, decreasing it s mechanical strength, as well as generating small amounts of extractable breakdown products. Like all conventional Polystyrene Type II anion resins, it is thermally stable to 77 oC (170 oF) in the salt form. The hydroxide form tends to degrade in water temperatures appreciably higher than 35 oC (95 oF), thereby losing capacity, as the functional groups are gradually replaced by hydroxyl groups.